METHOD FOR MANUFACTURING Bi-Te BASED p-TYPE THERMOELECTRIC MATERIAL

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 15 | 10-727391 | 2005-125919 | Korea Institute of Industrial Technology | H01L 27/16 |
| Registration 15 | 2007.06.05 | 2005.12.20 | Korea Institute of Industrial Technology | H01L 27/16 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a method for manufacturing a Bi-Te series p-type thermoelectric material by mixing coarse powder and fine powder at a predetermined mixture ratio and sintering the mixture by means of a spark plasma sintering process.

ㅇ	Thermoelectric devices made by casting such as unidirectional solidification or single crystal growth require high costs due to increases in manufacturing costs caused by yield reduction during processing and manufacturing.  Because of being easily split along a cleavage plane, a material of singe crystal is difficult to process and is much lost.

To solve the problem, this technology is an improved technology which removes conventional disadvantages by mixing coarse powder and fine powder at a predetermined mixing ratio, sintering the mixture by means of a spark plasma sintering process within a short period of time, e.g., within several minutes, in order to improve crystal orientation and facilitate texture densification and control, thereby providing a method for manufacturing a Bi-Te series p-type thermoelectric material that has superior mechanical strength and advantages in terms of performance and manufacturing cost.

ㅇ	The method according to this technology includes a vacuum sealing step S1 of weighing elements of Bi, Sb, and Te according to a p-type composition, charging corresponding elements into a quartz tube, and then vacuum-sealing the quartz tube, an ingot manufacturing step S2 of putting the quartz tube which is vacuum-sealed in step S1 into a stirring furnace for stirring, and applying furnace cooling in order to manufacture ingot, a crushing step S3 of crushing the ingot manufactured in step S2, a grinding step S4 of grinding the powder crushed in step S3, a dividing step S5 of dividing the powder grinded in step S4 into coarse powder having a grain size of 200~300㎛ and fine powder having a grain size of 20~45㎛ or less, a hydrogen reduction step S6 of charging the powders divided by the dividing step S5 into a pyrex tube, filling hydrogen into the tube, then sealing the tube, and heating and maintaining the tube at a predetermined temperature to reduce the hydrogen of the powders, a mixing step S7 of mixing the coarse powder and the fine powder passing through step S6, charging the mixture into an ample, vacuum-sealing the ample, and mixing the mixture by using a 3D mixer, and a sintering step S8 of sintering the powders mixed in step S7 by means of spark plasma sintering equipment.

3. Characteristics and/or advantages of the technology

This technology exhibits a relative density of 97% or higher, which means that gaps between coarse powders are filled with fine powders, and increases carrier mobility by improving sintering and orientation when compared to sintering using only fine powders, thereby having a feature of maximum performance index.

This technology increases bending strength by 3 times or more as a mixing rate of fine powder increases.

According to this technology, electric resistivity increases.  Although carrier density and thermoelectric power hardly change with a mixing rate of fine powder increases, heat conductivity slightly increases with an increase in the mixing rate and the increase of the heat conductivity is in inverse proportion to electric resistivity.  In other words, this technology facilitates densification of thermoelectric material texture and control of crystal grain size and thermoelectric performance, makes it possible to implement superior mechanical strength, and is advantageous in terms of performance and manufacturing cost.

4. Applicable market and use of the technology

This technology relates to a thermoelectric material that is an energy conversion material in which electric energy is generated by temperature difference between both ends of the material and temperature difference between the both ends is generated by electric energy applied to the material.  Presently, heat-electricity conversion is a thermoelectric module made of n-type and p-type semiconductor thermoelectric materials, which operates as an electric dynamo by being given temperature difference or operates as a cooler by electric current flowing along the thermoelectric module.  Thermoelectric power generation can generate electric powder by merely being given temperature difference, has a simple structure, generates no noise, and has a wide selection range of heat sources to be used.  For these reasons, thermoelectric power generation has already come into common use as special power source devices for remote places, the seabed, the universe, and the military.  Large-scale thermoelectric power generation technologies using various industry waste heat or natural energy are under development.  Thermoelectric cooling has a simple structure without having an operation part, has high thermal responsitivity strength and causes no noise or vibration.  Moreover, since selective cooling of fine parts is possible, thermoelectric cooling is used for fine temperature control or computer-related small-size coolers in semiconductors, laser diodes, and infrared detection devices.  Such applications will be expanded in future and applications for small-size refrigerators or warmers which do not use refrigerants attract much attention for the protection of environment.