Apparatus and Method for manufacturing FCCL (Flexible Copper Clad Laminate) film

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 82 | 10-661456 | 2005-70844 | Korea Institute of Industrial Technology | B32B 15/08B32B 15/20 |
| Registration 82 | 2006.12.19 | 2005.08.03 | Korea Institute of Industrial Technology | B32B 15/08B32B 15/20 |
| Representative Fig. |

2. Summary of the technology

This technology relates to a FCCL(Flexible Copper Clad Laminate) film, which is a basic constituent of a FPCB(Flexible Print Circuit Board).

FCCL film is an important basic constituent of FPCB used to produce mobile phone, LCD, digital camera, and etc. For forming large-scale of a circuit pattern for a mobile phone or digital products, a number of layers of FCCL film are used, and thus, copper plating layered on both surfaces of FCCL film is needed. However, because the copper plating apparatus and cleansing apparatus that are used for manufacturing conventional FCCL film is the method of forming the copper plating layer on one surface of a polyimide film, there are problems of low productivity and efficiency for manufacturing the FCCL film having copper plating layer on both surfaces.

On the other hand, this technology is a devised technology of an FCCL film to effectively provide electro-plate copper plating layer on both surfaces of a polyimide film by using a pair of current delivery rolls as a body of the positive current and jigs as a body of the negative current to be arranged in apposite directions in a plating bath for raise the productivity and efficiency.

An FCCL film manufacturing apparatus of this technology, while the films formed on the both surfaces transferred, wherein the copper plating layers are continuously plated on both surfaces of a film, is composed of an acid cleaning device(1) spraying an acid cleaning solution on both sides of a film(F) to be plated to remove an oxidation film from a copper film and depositing the film plural water cleaning devices(2a, 3b, 3c) spraying a water cleaning solution on the film to wash the acid cleaning solution and a copper electrolyte remaining on the film and depositing the film at least one copper plating device installed between the water cleaning devices to plate a copper plating layer on both sides of the film by supplying the negative current by coming into contact with the transferred film and feeding the positive current to a transfer path of the film dipped in the copper electrolyte a rust-proofing device(4) spraying a rust-proofing solution on the copper plating layer to prevent the copper plating layer from getting rusty while passing through the plating devices and a dryer drying the rust-proofing solution applied on the film.

3. Characteristics and/or advantages of the technology

This technology characterized in that a copper plating apparatus, which is included in the FCCL film manufacturing apparatus according to this technology, is effectively provided to electro-plate copper plating layers on both surfaces of a polyimide film by using a pair of current delivery rolls as a body of the positive current and jigs as a body of the negative current to be arranged in apposite directions in a plating bath.

This technology also features that an acid cleaning device and water cleaning devices included in the apparatus of this technology have plural couple of spraying nozzles installed in moving sidewall spraying an acid cleaning solution on both sides of a film to effectively remove remaining impurities, and are easy for maintenance or repair by control the location of the moving sidewall.

4. Applicable market and use of the technology

This technology relates to an FCCL(Flexible Copper Clad Laminate) film, which is a basic constituent of a FPCB(Flexible Print Circuit Board), more particularly to an FCCL film manufacturing apparatus and a method having copper plating layers on both surfaces of a film.

The need of the FPCB is increasingly extended for the tendency of slim-sized printing circuit board according to the small-sized and light-weighted electronic products. The main use of FPCB is applicable to mobile phone, digital camera, camcorder, computer or its peripheral devices, video, audio equipments, printer, DVD, TFT LCD, PDP, satellite equipments, military equipments, and medical instruments.