WAVEFORM CONTROL METHOD FOR GMA HIGH SPEED WELDING

1. The information of the patent

| Dowon International Administration No. | Publication No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 41 | 10-668233 | 2006-16048 | Korea Institute of Industrial Technology | B23K 9/09 B23K 9/08 |
| Registration 41 | 2007.01.08 | 2006.02.20 | Korea Institute of Industrial Technology | B23K 9/09 B23K 9/08 |
| Representative fig. |

2. Summary of the technology

This technology relates to a waveform control method for GMA high speed welding.

Generally, it is important for CO₂ high speed welding to raise the electric current and lower the voltage to thereby raise the short-circuit ratio. However, there have been problems when the welding voltage is set up at the low point, during short-circuit the rising current is lowered and arc is not generated, so the stubbing phenomena hitting to the melting pool is generated, and under cut or humping bead is generated by the phenomena of instant short-circuit and long-pending arc.

This is a devised technology to avoid afore said problems by providing waveform control method for GMA high speed welding to stably progress the GMA high speed welding by keeping the current rising gradient during the short-circuit.

This technology of a waveform control method for GMA high speed welding, wherein the control of waveform for high speed welding accompanying short-circuit transfer by alternately generating the short-circuit and arc phenomena, comprises a first control step of guiding the rapid solution of the short-circuit by keeping the current rising gradient of the 150~300 A/ms welding current during the short-circuit; a second control step of delaying 8~12 ms after the arc is generated by the afore said first control step; and a third control step of guiding the short-circuit by reducing 40~60 A current after the time delay by the afore said second control step.

3. Characteristics and/or advantages of the technology

This technology characterized in that accelerating the short-circuit by reducing electric current after the time delay of the arc generation.

This technology also features that keeping more than determined length of arc by rapid arc regeneration during short-circuit by melting speed of a wire raised to thereby quick arc is regenerated for reduce the subbing phenomena that a wire is stucked up in the melting pool by controlling the short-circuit current rising gradient.

When a waveform is controlled according to this technology, more desirable welding bead is attainable(or accomplished), and the high speed welding of 2~3.5 m/min is possible.

By the control of welding current according to this technology, it is possible that stable GMA high speed welding by reducing the stubbing, instant short-circuit, and long-pending arc phenomena generated during high speed welding. And also, it is possible to raise the productivity and according to this, it has an advantage of cost reduction when a thin plate is being welded because of possibility of stable high speed welding.

4. Applicable market and use of the technology

This technology relates to welding, the welding is directly related to design and production of a structure, and as one of the major joining technology, it is applicable to a large field of present industries. And also, it relates to welding material, welding technique, and welding dynamics, and it includes GTA, GMA, CO welding, general welding, welding metallurgy, special welding and destruction or non-destruction of welding design or welding portion's heat flow. GMA welding has an advantageous thing that it doesn't generate slag, therefore it is settled as the most suitable technique in the tendency of welding automation. Recently, there has been a tendency that semi-automatic FCA(Flux Cored Arc) welding is replaced by GMA(Gas Metal Arc) welding because of the extension of robot welding and mechanized welding in the domestic country.

The welding industry roughly can be divided into welding machine and material industry and welding construction industry, however, the representative productions of the welding machine and material industry are welding material and welding machinery. And, welding shearing machinery, welding automation machinery, and system production industry are included in the welding machine and material industry. Welding machine and material is used to make many kinds of structures of shipbuilding, vehicle, chemistry facility, electric home appliances, construction, bridge, and so on. The welding machine and material industry is the foundation industry to supply welding materials and machineries for national infra-structure industry of heavy industry, vehicle, construction, electric home appliances and so on. Therefore it has major industrial advantage of having forerunning effect in the related industry aspect.