HEAT RESISTANT CASTING MAGNESIUM ALLOY

1. Information of the patent

| Dowon International Administration Nos. | Registration Nos. | Application Nos. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration Nos. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 103 | - | 2005-126591 | Korea Institute of Industrial Technology | ? |
| Application 103 | - | 2005.12.21 | Korea Institute of Industrial Technology | ? |
| Application 104 | - | 2006- 1602 | Korea Institute of Industrial Technology | ? |
| Application 104 | - | 2006.01.06 | Korea Institute of Industrial Technology | ? |
| Representative Figs. |

2. Summary of the technology

ㅇ	This technology relates to a heat resistant casting magnesium alloy having high-temperature rigidity as well as similar normal-temperature rigidity and corrosion resistance to those of  common-use magnesium alloys of AZ series.

ㅇ	Existing alloys of Mg-Al-(Zn) series undergo rigidity degradation at high temperatures, limiting their uses to environments at temperatures of 102 ℃ or less.  To solve this problem, studies have been conducted to add various alloy elements.  However, in most cases, since expensive elements such as rare earth elements are much added, there are many restrictions in use and castability may degrade due to the added elements.	On the other hand, this technology is an improved technology which adds Zn or Ca in order to improve heat resistance while maintaining capability, mechanical features, and price.

ㅇ	The heat resistant casting magnesium alloy of this technology is composed of Al 6.0~9.0 wt.%(6.0 to 9.0 wt.% of Al), Zn 4.1~6.7 wt.%, Mn 0.1~1.0 wt.%, and inevitable impurities as the remaining element, or Al 6.1~8.5 wt.%, Ca 0.45~1.84 wt.%, Mn 01~1.0 wt.%, and Mg including inevitable impurities as the remaining element.

3. Characteristics and/or advantages of the technology

The heat resistant casting magnesium alloy of this technology is advantageous in that it has mechanical features, corrosion resistance, and capability that are similar to those of common-use magnesium alloys of Mg-Al-(Zn) series, and also has high-temperature rigidity.

4. Applicable market and use of the technology

The applicable market of this technology is the magnesium alloy market.  Magnesium alloys, which are light-weight alloys having high specific strength, can be sheet-molded by means of normal casting and high-pressure casting and has electromagnetic shielding effects.  Moreover, in the field requiring heat resistance, heat resistant magnesium alloys can be manufactured without expensive rare earth elements.  For these advantages, this technology can be applied to a wide range of fields such as the aerospace field(as materials for rockets or aircrafts), the vehicle field, the sports and leisure field(as materials for bicycles and the like), the information and communication field(as materials for digital cameras, cellular phones, and notebook cases.