NICKEL HYDROGEN BATTERY

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 28 | 10-787104 | 2006-130214 | Korea Institute of Industrial Technology | H01M 10/38 H01M 10/02 |
| Application 28 | 2007.12.12 | 2006.12.19 | Korea Institute of Industrial Technology | H01M 10/38 H01M 10/02 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to nickel hydrogen batteries with improved charging efficiency and extended lifespan.

ㅇ	Existing nickel hydrogen batteries had charging efficiency of at most 85-90% and was problematic in that gases and electrolyte of the batteries were leaked when being fully charged.  Accordingly, the existing nickel hydrogen batteries were problematic in that they had a short lifespan and safety problems, such as the explosion of gases within the batteries, because electrolyte was reduced to thereby degrade the performance abruptly.

In contrast, this technology is an improved technology with an extended lifespan and improved charging efficiency through change of constitutions of alloy and addition of additives.

ㅇ	The nickel hydrogen batteries of this technology relates to a technology including a cathode having hydrogen-storing alloy in which the amount of La ranges from 25 to 80 wt%; and an anode having hydration nickel which is coprecipitated or has its surface improved by additives including Co, Zn, Ca and Mg.

3. Characteristics and/or advantages of the technology

The nickel hydrogen batteries according to this technology has an equilibrium hydrogen pressure decreased by increasing the contents of La of Mm(Misch metal: La 15-20%, Ce 40-55%, Pr 3-15%, Nd 10-25%) in MmNi5-based alloy, that is, a conventional cathode material, and is characterized in that the amount of La of the hydrogen-storing alloy is 25 to 80 wt% of a total amount and charging efficiency is increased to about a level of 95% when compared with the existing nickel hydrogen batteries.  Meanwhile, hydration nickel constituting the anode is characterized in that the occurrence of oxygen by coprecipitating or having its surface improved by additives including Co, Zn, Ca and Mg and is advantageous in that it has an extended lifespan by improving a short lifespan depending on the shortage of electrolyte by reducing the occurrence of internal gases and prohibiting the emission of gases.  The nickel hydrogen batteries according to this technology is also advantageous in that it can prevent explosion due to an abrupt increase of internal pressure, which is caused by internal short or other factors, by mounting a safety bent unit therein.

4. Applicable market and use of the technology

This technology relates to nickel hydrogen batteries and can be applicable to the nickel hydrogen battery market.  Nickel hydrogen batteries enable high capacity, endure overdischarge and overcharge, and has a lot of charging numbers and is therefore used widely.  The nickel hydrogen batteries of this technology has an extended lifespan and improved charging efficiency compared with the existing nickel hydrogen batteries and can be used as batteries for portable phones, notebook computers, small-sized audio cassettes, handy cams, etc. as well as electric cars, hybrid car, etc.

This technology can also be applicable to fields requiring clean products such as communication signals, power storage and emergency power because it can prevent contamination due to the leakage of electrolyte.