METHOD OF FABRICATING RFID TAG, RFID TAG AND ELECTRICAL CONNECTION MEMBER FOR RFID TAG

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 70 | - | 2006-125624 | Korea Institute of Industrial Technology | G06K 19/07 |
| Application 70 | - | 2006.12.11 | Korea Institute of Industrial Technology | G06K 19/07 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a RFID tag(Radio Frequency Identification tag) that is widely applied to credit cards, ID cards, management tags of products, and so on.

ㅇ	A general antenna end connection member includes metal foil, and a crimping member of a type that grips the front and back of both ends of an antenna coil layer.  This method was problematic in that electrification members must be used on both sides.  This may cause short between conductors, so electromagnetic waves may be scattered.  Further, another type of an antenna connection member is formed using a method of forming an insulating layer on an antenna coil layer, etching via holes in the insulating layer at both ends of the antenna, and gap-filling the via holes with an electrical conductive material in order to connect the electrical conductive material to metal foil.  The antenna connection member was problematic in that the process was complicated and harmful chemical substance was used a lot during the process.

This technology is an improved technology which can form an antenna closed loop simply and can provide a RFID tag with high reliability and an electrical connection member for a RFID tag.

ㅇ	This technology is a technology regarding a method of fabricating a RFID tag, including the steps of forming an antenna coil layer at both ends; and forming an antenna end connection member to connect both ends of the antenna coil layer so that the antenna coil layer forms a closed loop, wherein the antenna end connection member includes metal foil, and an anisotropic conductive adhesive film intervened between the metal foil and both ends of the antenna coil layer.

3. Characteristics and/or advantages of the technology

This technology is characterized in that it can fabricate a RFID tag simply and rapidly since a subsequent process can be performed by adhering an integrated anisotropic adhesive film to the metal foil.

This technology is advantageous in that reliability of products is high and RFID tags with a high production yield can be fabricated since this technology is environment-friendly and does rarely generate metal short, etc.

4. Applicable market and use of the technology

This technology is a RFID tag technology, which is an apparatus that automatically updates information while exchanging the information with a chip and an external device, for example, a reader through an antenna in a non-contact state.  This RFID tag can be applied to credit cards, ID cards, management tags of products, and so on in various ways.

In general, the RFID tag of this technology can replace bar code used for article management in the distribution field.  That is, if the RFID tag technology is employed in the distribution field, a micro-chip containing information about the entire process of production, distribution, stock and consumption can be built by attaching a RFID tag to products.  A reader can track corresponding information through an antenna using a radio frequency.