Ti-BASED ALLOY MATERIAL WITH LOW MODULUS OF ELASTICITY AND EXCELLENT BIOCOMPATIBILITY AND MANUFACTURING METHOD THEREOF

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 49 | 10-653160 | 2005-23281 | Korea Institute of Industrial Technology | C22C14/00C21D 8/00 |
| Registration 49 | 2006.11.27 | 2005.3.21 | Korea Institute of Industrial Technology | C22C14/00C21D 8/00 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a titanium alloy material suitable as an artificial bio-material.

ㅇ	Conventional stainless steel and cobalt alloy materials are apt to corrode, causing diseases and destroying osseous tissues.  Various titanium alloy materials have been developed to solve the problems, but are toxic or cause stress shielding due to higher elastic coefficient than human bones, resulting in another surgical operation.

On the other hand, this technology is an improved technology which has a similar elasticity to human bones, and prevents stress shielding and has similar mechanical properties to living bodies for improvement of biocompatibility.

ㅇ	Low-elastic coefficient titanium alloy material having superior biocompatibility according to this technology is composed of niobium(Nb) of 10 ~ 30 at% that is an alloy element having no cytotoxic and having superior biocompatibility, silicon(Si) of 0.1 ~ 2 at%, oxygen of within 0.5 at% including impurities, and the remaining titanium(Ti) relative to total alloy weight.

3. Characteristics and/or advantages of the technology

This technology relates to a titanium alloy material suitable for use as artificial bio-materials(implant) such as artificial bones, artificial joins, and artificial tooth, and has similar rigidity and tensile strength to living bodies without harmful elements to the living bodies.

A titanium alloy material obtained according to this technology has high biocompatibility because of being composed of high corrosion-resistance and non-toxic elements, and can prevent stress shielding because of having a similar elastic coefficient of 45~55 GPa to an elastic coefficient of 10~40 GPa of human bones.

According to this technology, a low-elastic coefficient titanium alloy material having a similar elastic coefficient to that of human bones is obtained by dissolution processing and thermal processing, and can be shaped in linear, bar, and board forms by using typical processing methods such as rolling, pressing, and imprinting.

4. Applicable market and use of the technology

This technology relates to a titanium alloy material suitable for an artificial bio-material and its applicable market is the implant market such as artificial joints, artificial bones, and artificial tooth.  Implant is used to restore failed parts such as joints or tooth of human bodies, and thus the titanium alloy material can be used as implant products in the medical field such as orthopedic surgery, plastic surgery, and dental surgery.