SHOCK ABSORBER USING THE MAGNETIC FLUID

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 8 | 10-660390 | 2005-31753 | Korea Institute of Industrial Technology | F16F 9/53 |
| Registration 8 | 2006.12.15 | 2005.04.18 | Korea Institute of Industrial Technology | F16F 9/53 |
| Representative Fig. |

2. Summary of the technology

This technology relates to a shock absorber using the magnetic fluid, a shock absorber being originally used to reduce the shock or alleviating vibration, which can vary repulsive force and indicate its relative location by changing the viscosity of the magnetic fluid as to the amount of the applied shock or vibration.

This technology is provided by laminating repeatedly an insulator and a permanent magnet in a cylinder's inner part vertically formed on the upper portion of a piston and by laminating repeatedly an insulator and a subsidiary coil in a piston rod in the piston to form magnetic energy generating means. However, it has been a problem that electromotive force of a permanent magnet and a subsidiary coil generated by the shock or vibration(relative movement of a cylinder and a piston rod) of a moving vehicle cannot be easily perceived its direction and volume. In addition, a cylinder is long vertical shape and a coil is located in the inner lower portion of the cylinder, therefore, the heat(magnetic energy) generated from coil cannot reach to the upper portion of the magnetic energy generating means that is comprised of a subsidiary coil and a permanent magnet. And as a magnetic fluid, which is filled in the inner portion of a cylinder, since the viscosities of the magnetic fluid located in the upper portion and lower portion are different each other, a piston is adjusted to the movement of the shock and vibration(relative movement of a cylinder and a piston rod), and is not operated effectively, therefore it causes the problem of reducing attenuation. And, if the position of a permanent magnet installed in the inner cylinder and a subsidiary coil installed in the piston rod are not formed to be correspond each other in a exactly same position, it is impossible to set the working range of a piston exactly, and reduce the attenuating function because of change of viscous magnetic fluid.

Therefore, this technology is an improved technology using the magnetic fluid, avoiding the afore said conventional problems by placing a piston in the inner portion of a cylinder filled with a magnetic fluid, a piston rod that is circulated through the middle of the upper surface of the cylinder therethrough is integrally formed on an upper surface of the piston, power is supplied to the coil of the piston through the piston rod, but the piston rod integrally mounted on the upper surface of a piston is alternately accumulated with a permanent magnet and an insulator, and a Hall sensor is installed on an outer surface of the piston rod composed of those permanent magnet and insulator by using magnetic fluid.

This technology using the magnetic fluid comprises a tubular type cylinder(11) filled with a magnetic fluid(15); a piston(12) vertically moving in the cylinder; a coil(13) formed with the piston; plural guide rails(14) vertically installed on an outer surface; a piston rod(16) integrally formed on an upper surface of the piston and inserted in the middle of a cover(11-1) and protruded to an upper side; and a wire installed on the center line to supply power with the coil of the piston. The piston rod mounted on the middle of the upper surface of the piston accumulates alternately a permanent magnet(17) and an insulator(18). A sensor(19) is installed to sense the permanent magnet alternately accumulated with the insulator, wherein the sensor is a hall sensor.

3. Characteristics and/or advantages of the technology

This technology characterized in that the circulating amount of a permanent magnet forming a piston rod can be perceived via a sensor operated by the shock or the vibration and the electrical current amount permitted to the coil is controlled to change of the viscosity of the magnetic fluid, as a result, the repulsive force can be variable.

This technology features that the circulating amount of a permanent magnet is perceived by a sensor, electrical current amount permitted to the coil is controlled, and the magnet field formed around a piston is varied to change the gel condition of the magnetic fluid, accordingly, irregularly and swiftly applied shock and vibration can be adjusted promptly and smoothly, and they are attenuated promptly. And it also features that a vehicle's condition according to passenger number and weight of load can be judged by a permanent magnet and a sensor.

4. Applicable market and use of the technology

This technology can be applicable to a motor and a vehicle using a shock absorber together with a spring that absorbs the shock. Especially, to dramatically improve safety and comfortableness of a vehicle, it can be directly applicable to a shock-relieving apparatus for absorbing a shock and vibration(intrinsic vibration) applied to a tire to thereby relieve the shock transferred to the vehicle's body.