AN ORGANIC-INORGANIC HYBRID NANOPOROUS ANION-EXCHANGE RESINS FOR THE TREATMENT OF WASTEWATER CONTAMINATED BY PERCHLORATE AND THE METHOD FOR PRODUCING THE SAME

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 9 | - | 2006-43534 | Korea Institute of Industrial Technology | B01J 41/00 B01J 41/02 B01J 41/04 |
| Application 9 | - | 2006.05.15 | Korea Institute of Industrial Technology | B01J 41/00 B01J 41/02 B01J 41/04 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to an anion-exchange resins for the treatment of wastewater contaminated by perchlorate.

ㅇ	Perchlorate has high mobility in soil and groundwater due to its high    solubility and remains for a long period of time because of low reactivity and affects human bodies with extremely small quantities.  Thus, development of a technology for processing perchlorate is urgently needed.  However, traditional ion-exchange resin has some disadvantages such as a need for regeneration, instability with respect to an oxidizing agent, volume expansion and deformation, and limitations such as influences from obstacle factors.	On the other hand, this technology is an improved technology which is added thereto a support and a functional group in order to improve absorptivity and solves the disadvantages and limitations of the traditional ion-exchange resin.

ㅇ	A method of manufacturing organic/inorganic complex nanoporous anion-exchange resin according to this technology includes first step of manufacturing a nanoporous support with a silica precursor and a structure derivative, and second step of combining 2 types of functional groups having different carbon bond lengths with the nanoporous support.

3. Characteristics and/or advantages of the technology

This technology relates to nanoporous anion-exchange resin and a manufacturing method thereof in order to effectively remove an anion contaminant, such as perchlorate, remaining in an aqueous solution with very low concentration.

Anion ion-exchange resin according to this technology is characterized in that ammonium functional groups having different chain lengths are combined with a nanoporous support manufactured using a silica precursor and a structure derivative.	Organic/inorganic complex nanoporous anion-exchange resin manufactured according to this technology is ion-exchange resin having a fast adsorption feature and can effectively remove anion contaminants such as  perchlorate from wastewater and process water.

4. Applicable market and use of the technology

This technology relates to anion ion-exchange resin for processing wastewater contaminated by perchlorate and its applicable market is the wastewater processing field.  Perchloric acid ammonium generating perchlorate is used as propellents for explosives, rockets, and jet engines.  For this reason, wastewater generated in these industrial fields is contaminated by perchlorate.

Anion-exchange resin according to this technology can be used to process wastewater in these industrial fields because of effectively removing perchlorate remaining with very low concentration.