CLUTCH USING THE MAGNETIC FLUID

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 5 | 10-593834 | 2005-25457 | Korea Institute of Industrial Technology | F16D 35/02 |
| Registration 5 | 2006.06.20 | 2005.03.28 | Korea Institute of Industrial Technology | F16D 35/02 |
| Representative Fig. |

2. Summary of the technology

This technology relates to a clutch that transmits or cuts off the driving force of a power source, and more particularly, to a clutch using a magnetism separation type magnetic fluid that transmits or cuts off the driving force according to the variation of viscosity.

This technology is provided to improve the problem found in conventional electronic or magnetic clutches that when they are used for a long period of time, they cause malfunctions, thereby lowering the manufacturing costs, improving the productivity thereof and preventing the environmental pollution.

According to this technology, there is disclosed a clutch using a magnetic fluid having a starting fly wheel 4 having an input shaft 2 fixed at the center of one side thereof, an inside case 5 mounted at the other surface of the starting fly wheel 4 and having a fluid chamber 11 formed at the inside thereof, a magnetic fluid 20 filled in the fluid chamber 11, a rotor 15 embedded in the fluid chamber 11, an outside cover 10 mounted sealed at the outside of the inside case 5, a rotor-integrated output shaft 3 coupled sealed at the center of the outside cover 10, an electromagnetic coil 21 mounted inserted along the outer periphery of the fluid chamber 11, and a cooling means formed on the outer surface of the inside case 5, thereby connecting or disconnecting the power inputted to the input shaft 2 with the output shaft 3, wherein the inside case 5 comprises a protruded ring 6-1 fixed at one side to the other side of the starting fly wheel 4, an inside fly wheel 6 fixed at one side to the other side of the protruded ring 6-1 and a cylinder 7 mounted at the other side of the inside fly wheel 6, and wherein a cooling chamber 8 is formed between the starting fly wheel 4 and the inside fly wheel 6 and the protruded ring 6-1, the cylinder 7 having the outside cover 10 mounted sealed at the outer periphery thereof.

3. Characteristics and/or advantages of the technology

According to this technology, there are some advantages in that the structure is simple to lower the production costs, the manufacturing process is easy to improve the productivity thereof, the adequate arrangement of the heat sink and the bearings prevents the generation of the heat (electricity) from the magnetic fluid, and the automatic gear oil is not needed to avoid the environmental pollution thereby.

According to this technology, as the power supplied to the electromagnetic coil is turned on or off, the viscosity of the magnetic fluid is varied by the magnetic field generated from the electromagnetic coil to hold or release the rotation of the rotor, thereby supplying or cutting the power inputted to the input shaft to or from the output shaft.  Further, a cooling pin is mounted at the outside of the inside fly wheel and the outside cover constituting the fluid chamber so as to rapidly remove the heat of the magnetic fluid, thereby basically preventing the generation of the malfunction.

4. Applicable market and use of the technology

This technology is widely applicable to general industrial machines like motors and automobiles using the clutch transmitting or cutting power to a driven shaft in the state where the motor is not halted.  Especially, this technology relates to an electric clutch in a variety of clutches like a friction clutch, a fluid clutch and the electric clutch, and also relates to the clutch using the magnetic fluid in the electric clutch having a magnetism separation type and an electronic disc type, such that the clutch can be effectively applied to the related technology fields.