COATER ROLLER FOR PREPARATION OF SOLID OXIDE FUEL CELL; and PREPARATION METHOD OF SOLID OXIDE FUEL CELL

1. Information of the patent

| Dowon International Administration Nos. | Registration Nos. | Application Nos. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration Nos. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 97 | 10-566135 | 2004-30171 | Korea Institute of Industrial Technology | H01M 8/00 |
| Registration 97 | 2006.03.23 | 2004.04.29 | Korea Institute of Industrial Technology | H01M 8/00 |
| Registration 98 | 10-578557 | 2004-25902 | Korea Institute of Industrial Technology | H01M 8/00 |
| Registration 98 | 2006.05.03 | 2004.04.14 | Korea Institute of Industrial Technology | H01M 8/00 |
| Representative figs. |

2. Summary of the technology

This technology relates to a coater roller for an apparatus for manufacturing an electrolyte and an electrode of a solid oxide fuel cell, and solid oxide fuel cell manufacturing method thereof to allow the massive production of a unit cell constituting a fuel cell, thereby improving the productivity of a fuel cell.

The conventional solid oxide fuel cell manufacturing methods have many problems in that continuous working is impossible to make product's quality uniformly, working speed is slow and they need high priced apparatus, therefore, the production and manufacturing cost get high, they also have defects of generating cracks, and so on.

On the contrary, this technology is a devised technology added a coater roller and automation progress for improving productivity, and having an excellent electric characteristic without having any defects.

The apparatus for preparing a solid oxide fuel cell comprises a plurality of supply pipes for supplying the corresponding slurry a plurality of coating device parts installed in the rear part of the supply pipes for coating the slurry and a plurality of driers and annealing furnaces installed in the rear part of the coating device parts to dry and annealing the slurry, wherein the each coating device part has a coater roller capable of rotating, and a plurality of grooves continuously formed on the outer circumference of the coater roller along circumference for coating the slurry (an electrolyte slurry, an air electrode slurry and a fuel electrode slurry); a method for preparing a solid oxide fuel comprised of sintered air electrode slurry and a fuel electrode slurry on both sides of the electrolyte layer formed through dry and annealing process, wherein the method comprises the steps of coating and dividing the electrolyte slurry and sintering the coated one to form an electrolyte layer coating the supplied air electrode slurry on the one side of the electrolyte layer and sintering the coated one to form an air electrode layer and coating the supplied fuel electrode slurry on the other side of the electrolyte layer and sintering the coated one to form a fuel electrode layer, to prepare a solid oxide fuel cell.

3.  Characteristics and/or advantages of the technology

This technology characterized in that a coater roller allows the each slurry to be distributed and coated uniformly without the defect of annealing to thereby preserve an excellent film's characteristic of a coated layer.

In addition, the manufacturing method of the each slurry of an electrolyte slurry, an air electrode slurry and a fuel electrode slurry is processed with automation method, and it allows the massive production of a unit cell constituting a fuel cell, thereby improving the productivity of a fuel cell. Therefore, this technology features that the method can dramatically lower the production and manufacturing cost to thereby raise the cost competitiveness and reliability of product.

4.  Applicable market and use of the technology

This technology can be applicable to markets of a fuel cell product or manufacturing apparatus, and a power generator. Fuel cell usages can be divided into a portable power generator for a mobile phone and a notebook computer, a power supplier of transportation for a vehicle, and an electric generator for a domestic cogeneration plant and a power plant. A solid oxide fuel cell, as one of the fuel cells, can be operated in the highest temperature and has simple structure. In addition, it features that it doesn't have problems of loss, supplement, and corrosion of an electrolyte and is easy to provide fuel, therefore, because of the advantages, it is called as a fuel cell of 3rd generation and is in the limelight as a source of energy in the future.

According to the manufacturing method of this technology, it is expected to contribute the development of the field of a solid fuel cell as a source of energy in the future, because the technology prevents the products from having defect, and can improve productivity with providing excellent characteristic.