METHOD FOR MANUFACTURING AN NANOSTRUCTURED COATING TARGET AND THE SAME PRODUCT

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 19 | 10-711833 | 2006-987 | Korea Institute of Industrial Technology | C23C 14/06 C23C 14/34 B22F 9/00 |
| Registration 19 | 2007.04.19 | 2006.01.04 | Korea Institute of Industrial Technology | C23C 14/06 C23C 14/34 B22F 9/00 |
| Representative Fig. |

2. Summary of the technology

This technology relates to a method for manufacturing a nanostructured coating target and the same product so as to develop a sputtering target or an arc ion plating target that is used in high speed machining tools.

In the conventional methods for manufacturing a target two or more kinds of targets are located in a chamber, such that there is a problem that the structure is more complicated in suitably determining a nanostructured coating process.  Since no uniform alloy is manufactured by using general casting methods, thus, a high quality of target material, which satisfies various conditions(that is, uniform distribution of ally components, high purity and density, grains having relatively small sizes, uniform size distribution, uniform fine structures and uniform composition distribution) for improving the properties of a final product, is imported from other countries.

According to this technology, a Ti-Al-Si alloy sintered material(target) having excellent physical properties is manufactured by means of mechanical alloying and spark plasma sintering and is used as a next generation nanostructured coating material in high speed machining tools.

The method for manufacturing a nanostructured coating target according to this technology comprises the steps of distributing elements Ti, Al and Si alloys uniformly in material powder by means of mechanical alloying and simultaneously fine-granulating the grains in the powder to nano sizes; and after the material powder obtained through the fine granulation is put, uniformly distributing the elements in the material powder by means of spark plasma sintering and simultaneously forming the grains in the powder as a nano-sized fine grained sintering material(target).

3. Characteristics and/or advantages of the technology

This technology is characterized in that after the material powder and balls in a weight ratio between 1:50 and 1:100 are mixed in a ball mill, mechanical alloying is carried out wherein the ball mill is rotated in a nitrogen or hydrogen atmosphere at a speed in a range between 200 rpm and 300 rpm for 10 through 100 hours.

Also, this technology is characterized in that the alloy elements of Ti, Al and Si are uniformly distributed in the material powder by means of the mechanical alloying and the spark plasma sintering, in that the grains of the material powder are granulated to a nano size of 20 nm or less, and in that the powder itself has a uniform size of 10 mm.  Therefore, this technology can provide the method for manufacturing a Ti-Al-Si alloy sintered material (target) having excellent physical properties.

Unlike the conventional manner where the TiAl target and the Si target are separately installed and coated, further, the Si is uniformly distributed in the TiAl alloy in this technology such that the nanostructure can be obtained with only a single target, thereby allowing a series of manufacturing processes to be simple and easy.

4. Applicable market and use of the technology

This technology can be useful in a variety of fields manufacturing automobiles, ships, and electronics requiring high speed and high performance in a cutting process.  This main characteristic of this technology is high speed machining.  As this technology is adopted to high speed machining cutting tool, next generation nanostructured coating material in the high speed machining tool is manufactured having excellent durability, corrosion resistance, oxidation resistance, toughness, and hardness, and the improvement of the productivity obtained by this technology enhances a company’s competitiveness.