COMPRESSION MOLD WITH VERTICALLY MOVING LOWER MOLD

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 70 | 10-530271 | 2002-87636 | Korea Institute of Industrial Technology | B29C 33/44 |
| Registration 70 | 2005.11.15 | 2002.12.30 | Korea Institute of Industrial Technology | B29C 33/44 |
| Representative Fig. |

2. Summary of the technology

This technology relates to a compression mold that is provided with a lower die movable upward and downward, thereby improving the productivity thereof.

This technology is provided to improve the following problems existing technologies have had: first, a very expensive ejector mechanism is needed since the lower die is fixed to a press, thereby causing the pin marks for fixing the ejector to be formed on the outer appearance of the product at the time of separating the product from the mold; second, an operating space between the upper die and lower die after finishing the molding is not sufficient, thereby making it difficult to separate the product from the compression mold; and third, it is difficult to rapidly move the product from the compression press.

Therefore, the compression mold according to this technology comprises a coupling pin mounted on the upper die and having a coupling pin protrusion a, a coupling ring mounted on the lower mold and having a coupling ring protrusion b slanted in such a manner as to be rotatable when contacted with the coupling pin protrusion and a through-hole through which the coupling pin is passed, a conical roller bearing adapted to gently rotate the coupling ring, and a coupling ring guide plate and a lower die support having a guide plate fixing recess adapted to limit an amount of rotation of the coupling ring in cooperation with a coupling ring ball mounted on the lower die.

3. Characteristics and/or advantages of the technology

This technology has an advantage of completing a series of compression molding processes at one time.  That is, after the compression molding of the press has been finished, the lower die is moved in a vertical and upward direction together with the upper die, thereby improving the productivity thereof, and the compressed molded product remains on the fixed flat plate on the press bed, without having any separate ejector mechanism, thereby reducing the production costs of the mold and also keeping marks formed by ejector pins from remaining on the molded product to obtain a good quality of molded product.  Additionally, an operating space is sufficiently made when the finished molded product is separated from the mold, and as the molded product is placed on the flat plate, it is easier to convey the molded product from the compression press.

4. Applicable market and use of the technology

This technology can be used to mold manufacturing and designing fields, and therefore, it can be widely applicable to a press manufacturing and selling company, a mold material and product selling company, a product design company and the like.