FABRICATION SYSTEM AND METHOD OF E-PAPER

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 55 | - | 2007-61610 | Korea Institute of Industrial Technology | G02F 1/167 |
| Application 55 | - | 2007.06.22 | Korea Institute of Industrial Technology | G02F 1/167 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a system and method for fabricating e-paper.

ㅇ	In general, e-paper was problematic in that particles were accumulated on a barrier rib of a panel upon fabrication and the particles are damaged due to several problems in the convey and control process of the particles.

This technology is provided by lowering the amount of an electric field in regions other than an electrode by forming an insulating layer at the bottom of a stamp other than the electrode so that a particle is adhered to near the electrode to which a relatively high electric field is applied.  In particular, this technology is an improved technology which can prevent damage to the particle by removing several problems, which may occur in the convey and control process of the particle by designing the stamp constituting a thin film insulating layer at the bottom of the stamp including the electrode.

ㅇ	The e-paper fabrication system and method of this technology includes a PC(10) for minutely controlling stages through a camera(50) for precision alignment; a microprocessor(20) for communicating information with the PC(10) and controlling a first variable high voltage module(31), a second variable high voltage module(32) and a third variable high voltage module(33) according to communicated information; the first variable high voltage module(31) for controlling an electric field of an electrode(91) of a stamp(90) according to information transmitted from the microprocessor(20); the second variable high voltage module(32) for controlling a second precision position controller(70) according to information transmitted from the microprocessor(20); the third variable high voltage module(33) for controlling an electric field of a third precision position controller(80) according to information transmitted from the microprocessor(20); a vision board(40) for controlling the camera(50) for precision alignment according to control information based on information received from the PC(10); the camera(50) for precision alignment, which is minutely controlled according to the control information of the vision board(40) and photographs micro alignment of the stamp(90) and produces micro alignment data; a particle(60) coated on the electrode(91) of the stamp(90) and is filled in a panel(85) on the third precision position controller(80); the second precision position controller(70) which contains the particle(60) and performs micro movement the third precision position controller(80) which supports the panel(85)and performs micro movement the panel(85) which is place on the third precision position controller(80), becomes a frame of e-paper and is filled with the particle(60); the stamp(90) for coating the particle(60), which is contained in the second precision position controller(70), on the electrode(91) and fills the particle(60) into the panel(85) placed on the third precision position controller(80); a first precision position controller(95) which minutely controls the stamp(90) and conveys the particle(60); and a distance sensor(96) which is controlled by the PC(10) and senses a moving distance of the stamp(90).

3. Characteristics and/or advantages of the technology

This technology features a stamp fabricated to overcome the problem that a conventional particle is damaged.  That is, this technology is provided by forming the insulating layer at the bottom of the stamp by fabricating the stamp using a transparent substrate for vision alignment so that the particle is adhered to near the electrode to which a relatively high electric field is applied.  Accordingly, the particle does not touch over the panel barrier rib unnecessarily.

This technology can improve the process by fabricating and replacing only an adequate stamp without a significant change in the overall system and is therefore advantageous in convenience and economy.  This technology is also advantageous in that it can easily enlarge and expand the fabrication equipment with the help of a combination of stamps.

4. Applicable market and use of the technology

This technology relates to a fabrication system of e-paper which makes feel paper without change and serves as paper, and can be utilized for mobile phones, PDA, advertisement boards, price display devices, etc. in various forms as well as electronic devices for paper replacement such as e-book, e-magazine, and electronic paper.  Representatively, there are a plate type, a book type, an overcoat type, a paper type, and the like.