NON-WOVEN OIL/WATER SEPARATING FABRIC MATERIAL COMPRISING PLASMA COATING LAYER, AND OIL/WATER SEPARATING FILTER COMPRISING THE SAME; and WOVEN OR KNITTED OIL/WATER SEPARATING FABRIC MATERIAL COMPRISING PLASMA COATING LAYER, AND OIL/WATER SEPARATING FILTER COMPRISING THE SAME

1. Information of the patent

| Dowon International Administration Nos. | Registration Nos. | Application Nos. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration Nos. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 85 | - | 2006-123040 | Korea Institute of Industrial Technology | B01D 39/00 |
| Application 85 | - | 2006.12.06 | Korea Institute of Industrial Technology | B01D 39/00 |
| Application 86 | 10-786678 | 2006-123041 | Korea Institute of Industrial Technology | B01D 39/00 |
| Application 86 | 2007.12.11 | 2006.12.06 | Korea Institute of Industrial Technology | B01D 39/00 |
| Representative Figs. |

2. Summary of the technology

This technology relates to an oil and water separation material having the surface processed with plasma, an oil and water separation filter containing the same material, and a method for manufacturing the same filter, so as to provide the oil and water separation characteristics to a fuel filter in a variety of transporting means and industrial machines on which an engine is installed.

With the development of high performance diesel engines, new studies on a pollutants separation and removal material in transporting fields have been increasingly made.  That is, the oil and water separation performance should be high, and synthetic filter materials are more popular than the pulp filters having the market occupation of 80 % or more.  Thus, there is a need for the change to the synthetic fiber non-woven fabric having more improved filtering efficiency such that the dust removal capacity is increased and having more improved durability.  Additionally, such the filter material having environment-friendly processing technology is needed over the world, while not giving any influence on existing properties.

Under the above state, the plasma surface treatment according to this technology overcomes the problems the conventional practices have had, while providing a filter material having an excellent oil and water separation efficiency.

According to this technology, there is disclosed an oil and water separation material that is made by allowing a non-woven fabric(or a woven fabric or a knitted fabric) containing polymer fibers to be subjected to plasma surface treatment so as to form a plasma-coated layer having a surface tension in a range between 3.0 x 10-2 J/m2 and 7.2 x 10-2 J/m2, thereby providing an oil and water separation property to the surface.

3. Characteristics and/or advantages of the technology

This technology is characterized in that excellent water repellency is provided having an amount of consumption of high priced C2F6 gas reduced.

This technology is characterized in that both of the water repellency and the oil repellency are excellent.

Moreover, this technology is characterized in that the oil and water separation performance for separating water from oil(that is, only the diesel fuel is selectively permeated, while having no permeation of water) and the durability against oil are excellent.

4. Applicable market and use of the technology

This technology has more excellent properties than the conventional fuel filters and an environment-friendly manufacturing method, such that it is useful as the fuel filter in a variety of transporting means and industrial machines.  Additionally, this technology is applicable to an oil absorbing material for absorbing the oil spilling on general road surfaces and water surfaces, which is completely different from existing oil absorbing materials, oil fences and oil mats.

Further, the oil and water separation material according to this technology is applicable to a liquid/liquid separation material, a transporting in-tank filter in automobiles, a spin-on type filter, a diaphragm material in electric/electronic industries, a gas/liquid separation material, an aerosol separation material in industrial machines, and an air purification material in a clean room.  Additionally, the material can be applied to all kinds of industrial filters.