METHOD FOR MANUFACTURING FUNCTIONAL FILM USING SUPER-HIGH MOLECULAR WEIGHT POLYETHYLENE RESIN CONTAINING NANO CLAY AND FUNCTIONAL FILM USING THE SAME

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 19 | - | 2006-134745 | Korea Institute of Industrial Technology | C08J 5/18 |
| Application 19 | - | 2006.12.27 | Korea Institute of Industrial Technology | C08J 5/18 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a functional film containing nano clay in polymer resin.

ㅇ	In order to make up for limitations and disadvantages of polymer that is an organic substance, there have been attempts to improve physical properties by introducing nano clay.  However, it is difficult to uniformly disperse nano clay within polymer and thus to obtain desired physical properties.

On the other hand, this technology is an improved technology which improves rigidity and a gas blocking feature by improving the dispersibility of nano clay.

ㅇ	A functional film manufacturing method according to this technology includes first step of melting polymer resin in low-molecular weight oil, second step of providing a nano-clay dispersed solution, third step of mixing and stirring a resultant of first step and a resultant of second step in order to manufacture a mixture solution, and fourth step of manufacturing a functional film by using the mixture solution of third step.

3. Characteristics and/or advantages of the technology

This technology relates to a polymer functional film and can manufacture a polymer functional film having improved gas blocking feature and rigidity.

This technology improves nano clay dispersibility in super-high-molecular  weight polyethylene resin by using low-molecular weight oil, thereby improving the gas blocking feature and rigidity of the functional film.

4. Applicable market and use of the technology

This technology involves a functional film using polyethylene resin and its applicable market is the functional film market.  The functional film has various usages for packaging such as zipper bags and food packaging materials, for graphics such as print plate making and labels, for optical uses such as polarizing materials for LCDs and PDPs, and for industrial uses such as adhesive tapes.

The functional film manufactured according to this technology has improved rigidity and gas blocking feature by uniformly dispersing nano clay in polymer, and thus is very suitable for packaging requiring such improved features.