SYSTEM FOR LASER-ROTARY ARC HYBRID WELDING AND METHOD FOR LASER-ROTARY ARC HYBRID WELDING USING THE SAME; and METHOD FOR LASER-ARC HYBRID WELDING OF GALVANIZED SHEET STEELS AND SYSTEM FOR LASER-ARC HYBRID WELDING OF GALVANIZED SHEET STEELS

1. Information of the patent

| Dowon International Administration Nos. | Registration Nos. | Application Nos. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration Nos. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 36 | 10-656682 | 2005-129626 | Korea Institute of Industrial Technology | B23K 28/02 |
| Registration 36 | 2006.12.06 | 2005.12.26 | Korea Institute of Industrial Technology | B23K 28/02 |
| Registration 37 | 10-751301 | 2005-129633 | Korea Institute of Industrial Technology | B23K 28/02 |
| Registration 37 | 2007.08.16 | 2005.12.26 | Korea Institute of Industrial Technology | B23K 28/02 |
| Representative Figs. |

2. Summary of the technology

This technology relates to a laser-rotating arc hybrid welding device and a welding method using the same device, thereby suppressing poor welding.

This technology is provided to improve some defects found in the conventional practices that a separate shaft is needed to control a torch height, thereby causing the system to be complicated and also causing the control of the system to be hard to generate a large amount of poor welding and that a welding wire is selectively adopted, thereby inconveniently accompanying the exchanging process of the welding wire.

According to this technology, there is disclosed a laser-rotating arc hybrid welding device comprising: an arc discharge part adapted to conduct arc discharge with respect to a welding part; a laser generating part adapted to radiate laser to the welding part; and a rotary part adapted to rotate the arc discharge part.

3. Characteristics and/or advantages of the technology

According to this technology, MIG(metal inert gas) welding prevents the oxidation and nitrification of the molten metal by using inert gas and conducts the welding process, while continuously supplying welding electrodes.  Further, the welding adopts a self-fluxing wire as an electrode, thereby advantageously permitting the allowance of the space around the welding portion to be ensured, and as the arc discharge part is also rotated, the welding range is enlarged to further increase the allowance of the space around the welding portion.

According to this technology, high speed welding is achieved and the welding for a relatively thick steel plate is carried out at one path by means of keyhole mode welding.  Also, the thermal deformation is rarely generated by means of the local heat input.

This technology conducts the hybrid welding by means of laser and arc, wherein the arc discharge part is rotated to a given radius and even if the welding wire having a length of 1.2 mm is adopted with respect to the welding part having a space between 1.5 mm and 2 mm, a heat source can be sufficiently supplied to the welding part, thereby conducting the welding without any control of the torch.  Further, the arc discharge part is rotated to improve the liquidity of the weld pool, thereby suppressing the poor welding like undercut.

4. Applicable market and use of the technology

This technology relates to a laser-rotating arc hybrid welding device and a welding method using the same device, and therefore, it is applicable to a welding device production company, or to a machine processing company or a ship industry company that makes products by using a welding method.

Moreover, the poor welding like undercut is reduced, thereby providing a high quality of welding and further providing a high quality of product, and therefore, this technology is introduced adequately to high value product-manufacturing companies.