METHOD FOR SURFACE MODIFICATION OF IMPLANT

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 30 | 10-603976 | 2003-22975 | Korea Institute of Industrial Technology | A61L 27/06 |
| Registration 30 | 2006.07.14 | 2003.04.11 | Korea Institute of Industrial Technology | A61L 27/06 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a method for modifying the surface of implant by giving bio-activity to the surface of bio-implant made of titanium or a titanium alloy.

ㅇ	Implant for bio-implanting has to be made of bio-compatible materials which have no toxicity, antigenicity, and carcinogenicity and also have mechanical compatibility and chemical compatibility with bone tissues such as high coherence and retention and high corrosion resistance during the use.  However, conventional implant is not satisfactory in terms of the compatibility and various attempts to solve this problem have also some problems.

This technology solves conventional problems by modifying the surface of conventional bio-implanting implant made of titanium or a titanium alloy.

ㅇ	A method for modifying the surface of implant according to this technology includes a blasting process for spraying sand grains onto the surface of implant in order to form an oxide film on the surface of implant made of titanium or a titanium alloy(at which the size of each sand grain is 20~250 ㎛  the spraying pressure of a blast gun is 1~5 atmospheric pressure, and an interval between the surface of implant and the blast gun is 5 cm) and a film forming process using anodic oxidation(at which an implant specimen is dipped in an electrolyte made by mixing H2SO4 of 0.1∼5 M and H3PO4 of 0.1∼5 M, and then voltages of 20∼80 V as a first level, 80∼120 V as a second level, 20~150 V as a third level, 150∼200 V as a fourth level, and 200∼250 V as a fifth level are sequentially applied).

3. Characteristics and/or advantages of the technology

Implant according to this technology solves mechanical problems regarding implant lamination and fixing, which are problems corresponding to an initial operation, by adding processing steps of blasting and oxide film formation.

In addition, a bio-compatible stable oxide film can be formed on the surface of implant, thereby exhibiting chemical advantages.

Furthermore, bioactivity can be provided with the implant surface having porosity like bone tissues, thereby improving reactivity and surface activity with respect to bodily tissues and thus providing bio-compatibility.

In conclusion, this technology has superior mechanical compatibility, chemical compatibility, and bio-compatibility over conventional implant.

Simple processing of this technology is also one of significant advantages of this technology.

4. Applicable market and use of the technology

Importance and interest of bodily tissue implant become more important research subjects than anything else to the human race, along with the development of bioengineering and bio industry.  In particular, competition for development of new materials, processes, and systems is keen all over the world because of a ripple effect on human welfare, future society, and economy.  It is urgent for internal colleges and universities, research laboratories, and the industrial field to secure basic technologies by training next-generation creative human power and picking out ideas.  For this end, join researches covering science, engineering, medicine, and clinic are essential.

Although this technology is widely used in the dentistry field, it also will make it possible to localize bio-implanting implant materials which still depend on importation.  Therefore, this technology will be a material in various industrial fields, and in particular, is useful in the dentistry and material engineering fields which study, develop and produce implant materials and titanium.