METHOD MODIFYING SURFACE OF KERATIN FIBER

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 87 | 10-584821 | 2004-18781 | Korea Institute of Industrial Technology | D06M 11/00 |
| Registration 87 | 2006.05.23 | 2004.03.19 | Korea Institute of Industrial Technology | D06M 11/00 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a method for modifying the surface of keratin fiber by removal of surface scale of keratin fiber by using Fenton reaction and protein protease.

ㅇ	The keratin fiber feels coarse to the touch due to scale on its surface and shrinks after being washed.  Among conventional processing methods for preventing shrinkage, a chlorinated shrink-proofing processing method generates a wettable organic halogen compound(AOX) that is harmful for environments, and a processing method using synthetic resin does not provide sufficient shrink-proofing and does not feel good to the touch.

On the other hand, this technology is an improved technology which improves felting property and adds thereto Fenton reaction and protein protease processing for soft touch sensation.

ㅇ	The method for modifying the surface of keratin fiber according to this technology includes a) attaching an anion surfactant onto the surface of keratin fiber by processing keratin fiber with the anion surfactant, b) injecting cation into the keratin fiber passing through a) in order to attach cation to the surface of keratin fiber, c) injecting an oxidizer into the keratin fiber passing through b) in order to remove scale through Fenton reaction between the anion and the oxidizer, and d) processing the keratin fiber from which scale is removed in c) with protein protease.

3. Characteristics and/or advantages of the technology

This technology solves problems of conventional shrink-proofing processing methods, i.e., removes problems regarding environments, improves shrink-proofing, and improves touch sensation.  Moreover, after dyeing, bright color and concentration improvement can be obtained and wetability is improved.

4. Applicable market and use of the technology

This technology relates to a method for improving the surface of keratin fiber, and can be applied to fiber manufacturing and fiber product fields, and natural fiber spinning and modification processes.

Although the keratin fiber has usually been used in bedding such as bedclothes and pillows, winter clothing, and fashion items, surface-modified keratin fiber according this technology will be used for  various fields by having improved shrink-proofing and soft touch sensation.