METHOD OF FABRICATING LUMINESCENT DISPLAY

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 56 | - | 2006-134690 | Korea Institute of Industrial Technology | H05B 33/10 |
| Application 56 | - | 2006.12.27 | Korea Institute of Industrial Technology | H05B 33/10 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a method of fabricating a luminescent display which can increase an overall emission efficiency when fabricating a flat panel display or lightings employing an OLED or LED.

ㅇ	A conventional luminescent display had low emission efficiency and consumed lots of power in order to increase luminance.  A problem according to this was that the lifespan of an organic luminescent device was shortened.  A microlens fabricated to solve this problem had an expensive fabrication cost and was difficult to have a large area.

The luminescent display fabrication method of this technology is an improved technology which has shortened the fabrication cost and turnaround time of a microlens and entirely improved emission efficiency of a luminescent display.

ㅇ	The luminescent display fabrication method of this technology includes loading a liquefied material constituting a microlens into an ink jet printer; forming the microlens by spraying the liquefied material on the substrate in an ink jet spray manner and hardening the liquefied material to thereby form a microlens.

3. Characteristics and/or advantages of the technology

This technology is advantageous in that it does not require expensive semiconductor process equipment and simplify the fabrication process by employing an ink jet printing method and therefore can greatly shorten the fabrication cost and turnaround time.

This technology is also advantageous in that it can easily fabricate a necessary microlens using various patterns even without a new mold.

Further, the luminescent display of this technology has improved emission efficiency and is advantageous in that it can overcome a lifespan shortened due to an excessive application of voltage.

4. Applicable market and use of the technology

This technology can be applied to increase an overall emission efficiency in luminescent displays or lightings with an improved display ability in bright places by reducing the reflection of external light.

If this technology is applied to a flat panel display such as notebook monitors, in particular, it can implement motion images since its response speed is about 30,000 faster than that of a LCD and can implement a wide viewing angle and high luminance since the flat panel display can emit light itself rather than a LCD that does not emit light itself.