METHOD FOR FABRICATING LIGHT MODULATOR; and LIGHT MODULATOR

1. Information of the patent

| Dowon International Administration Nos. | Registration Nos. | Application Nos. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration Nos. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 88 | 10-623522 | 2004-15919 | Korea Institute of Industrial Technology | G02F 1/01 |
| Registration 88 | 2006.09.06 | 2004.03.09 | Korea Institute of Industrial Technology | G02F 1/01 |
| Registration 89 | 10-623521 | 2004-15918 | Korea Institute of Industrial Technology | G02F 1/01 |
| Registration 89 | 2006.09.06 | 2004.03.09 | Korea Institute of Industrial Technology | G02F 1/01 |
| Registration 90 | 10-623520 | 2004-15917 | Korea Institute of Industrial Technology | G02F 1/01 |
| Registration 90 | 2006.09.06 | 2004.03.09 | Korea Institute of Industrial Technology | G02F 1/01 |
| Representative Figs. |

2. Summary of the technology

ㅇ This technology relates to a method of fabricating an optical modulation device for the optical industry by employing material with a non-linear optical characteristic and easily fabricating a number of and multiple diffraction gratings at the interface of a metal film and an electrooptic material film by employing a pattern mask.

ㅇ This technology has improved a disadvantage in that commercialization is difficult due to a slow response speed and problems in that an expensive high refraction prism must be used and miniaturization, high integration and mass-production of devices are difficult to realize due to a large prism.

ㅇ An optical modulation device of this technology is a technology including a first deposition step of depositing a metal film on a top surface of a substrate a second deposition step of installing a pattern mask in front of the metal film and depositing metal again to thereby form a diffraction grating; a step of sequentially stacking an electrooptic material film and a transparent electrode over the diffraction grating and a step of forming the electrooptic material film using an electrooptic polymer material which changes a surface plasmon resonance condition as the refractive index of the electrooptic material film is changed by the Pokels effect when voltage is applied to the metal film and the transparent electrode.

3. Characteristics and/or advantages of the technology

This technology can have an effect in that it can easily implement a single, a number of and multiple diffraction gratings at the interface of the metal film and the dielectric material by employing the pattern mask. Thus, this technology is characterized in that it can solve the problems of the existing method employing a high refractive prism and implement an optical modulation system employing micro diffraction grating-coupled surface plasmon resonance.

This technology is advantageous in that it can easily realize simplification, miniaturization, high integration and mass-production through a low fabrication cost when compared with the Kretschmann type surface plasmon optical modulator required by the existing high refractive prism.

4. Applicable market and use of the technology

This technology can be applied to fabricate ultra-high speed optical switches, optical modulators, spatial-optical modulators, optical interconnects, optical filters, display and can also be largely applied to fabricate various components such as optical communication and information electronic fields.