METHOD OF MANUFACTURING SELF-AGGREGATION NANO DELIVERY VECTOR HAVING REVERSIBLE TEMPERATURE SENSITIVITY

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 44 | - | 2007-52774 | Korea Institute of Industrial Technology | C07D |
| Application 44 | - | 2007.05.30 | Korea Institute of Industrial Technology | C07D |
| Representative Fig. |

2. Summary of the technology

ㅇ This technology relates to a drug delivery system capable of executing an effective drug delivery function while having bio-friendliness and temperature sensitivity.

ㅇ This technology solves problems of conventional technologies, i.e., a limitation in the application as drug delivery systems because of disability to pass a plasma membrane due to large particle size; a difficulty in guaranteeing stability in a drug-captured state due to sensitivity to temperature change, molecular motion, etc.; and unsuitableness for use in drug delivery because the needle may be stopped up during injection due to temperature sensitivity.

ㅇ This technology involves a copolymer manufacturing method including (i) polymerizing a temperature-sensitive polymer; and (ii) causing 0.1~50 μmol of the temperature-sensitive polymer polymerized in (i) to react with 0.1~100 μmol of a hydrophilic polymer in order to generate a copolymer or a drug delivery vector manufacturing method including (i), (ii), (iii) adding drug to an aqueous solution of the copolymer generated in (ii); and (iv) capturing the drug by increasing temperature to a lower critical temperature or higher.

3. Characteristics and/or advantages of the technology

According to this technology, a drug delivery vector composed of a temperature-sensitive polymer having a lower critical temperature and a copolymer having hydrophilic natural polysaccharide exhibits particle formation and emission behavior reversibly according to temperature change.  Therefore, formation of drug delivery vector particles is controlled by temperature adjustment, thereby being able to be used as an efficient drug delivery vector providing easy drug capturing and emission.

Because of having a nano-level particle size by limiting the reaction rate of copolymer reaction, the drug delivery vector according to this technology can effectively delivery drug regardless of destination by passing a plasma membrane of an organism.  Moreover, by maintaining a particle state constant regardless of temperature change by means of bridging on the surface of the drug delivery vector according to this technology, the stability of a drug-captured state can be improved.

4. Applicable market and use of the technology

This technology can effectively fill various hydrophobic drug and therapeutic protein used for treatment or prevention of diseases and thus can be variously used as a medical drug delivery vector in the field of drugs and medications.