METHOD OF FABRICATING FILM WITH IMPROVED OPTICAL LUMINANCE FOR HIGH LUMINANCE OF LCD AND IMPROVED OPTICAL LUMINANCE FILM

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 65 | 10-793927 | 2006-120489 | Korea Institute of Industrial Technology | G02B 5/ 02 G02F 1/1335 |
| Application 65 | 2008.01.04 | 2006.12.01 | Korea Institute of Industrial Technology | G02B 5/ 02 G02F 1/1335 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a method of fabricating a film with improved optical luminance, which is mounted and used in a LCD and a film with improved optical luminance thereof.

ㅇ	In general, in a wedge-shaped improved optical luminance film, the intensity of light at 0 degree is the strongest and the intensity decreases as the angle increases when a vertical direction is 0 degree according to a 2-dimensional simulation, and light incident at an angle of about plus and minus 30 degrees or more has a reduced straight property.  Thus, the wedge-shaped improved optical luminance film was problematic in that it could not secure luminance and a viewing angle required for a LCD.

This technology relates to a method of fabricating a film with improved optical luminance and a film with improved optical luminance thereof, in which the surface of a sheet is formed in a spherical lens of an embossing form, wherein an additional engraving mold plate is fabricated in order to stamp and fabricate it using a stepper method and a film resin is stepped using the mold plate.

ㅇ	A method of fabricating a film with improved optical luminance for a LCD, of this technology includes the steps of molding a first plate using glass or silicon, wherein a bead groove having a diameter of 1-100 ㎛ is formed on a top surface of the first plate, fixing a bead to the bead groove formed in the first plate, wherein the bead is fixed to the bead groove through a self assembly method or a binder, fabricating a mold plate through electroplating or electroless plating by employing metal on a top surface of the first plate to which the bead is fixed, and stepping the mold plate into the film resin using a stepper, wherein when the mold plate is pulled off from the first plate, the mold plate has an engraving shape of a spherical lens.

3. Characteristics and/or advantages of the technology

This technology is characterized in that it can control optical efficiency effectively and provides high luminance and a wide viewing angle required in a LCD.

This technology is advantageous in that it can provide a high-definition image quality and save consumption power, and also has a low fabrication cost, enables mass-production and can shorten a task time because an improved optical luminance film is fabricated through the stepping process more easily.

4. Applicable market and use of the technology

This technology is a technology regarding an improved optical luminance film which can minimize optical scattering of an optical film rather than increasing the intensity of a light source and increase optical efficiency.  This technology is provided by forming a sheet a spherical lens of an embossing form, fabricating an additional engraving mold plate in order to stamp and fabricate the mold plate using a stepper method and stepping film resin using the mold plate, thus improving optical luminance.

If the improved optical luminance film fabricated by this technology is employed, optical efficiency can be controlled effectively and high luminance and a wide viewing angle can be provided.  Accordingly, a high quality of a LCD can be fabricated.