CONDUCTIVE PASTE COMPOSITION

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 69 | 10-786758 | 2006-125620 | Korea Institute of Industrial Technology | C08K 9/04 C08K 9/02 |
| Application 69 | 2007.12.11 | 2006.12.11 | Korea Institute of Industrial Technology | C08K 9/04 C08K 9/02 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a conductive paste composition.

ㅇ	Generally used conductive pastes include silver, copper, nickel, carbon, and the like and are used by dispersing them in a polymer solution.  Such conductive pastes have longitudinal stability such as electric features, physical features, heat resistance, water resistance, and the like.  However, since an oxide film is easily formed around a metal terminal or a gold terminal over time, instrument or video media cannot maintain high audio and video qualities, resulting in performance degradation.

This technology is an improved technology capable of providing a conductive paste which is environment-friendly by being composed of ‘silver powder’ and ‘squalene’ that is unsaturated hydrocarbon and gives electric features while suppressing formation of an oxide film when used in a metal terminal or a gold terminal of high-end electronic appliances or electric appliances.

ㅇ	The conductive paste composition of this technology is composed of ‘silver powder’ of 50~60 wt% and unsaturated hydrocarbon ‘squalene’ of 40~50 wt%.

3. Characteristics and/or advantages of the technology

Squalene constituting this technology is animal oil having an extremely low coagulation point, helps cell activation, and is characterized in that a conductive filler(silver powder) is given conductivity by adhering the conductive filler closely to a conductive portion such as a metal terminal and chaining conductive particles at the same time and then is given physical and chemical stabilities.

The conductive paste composition according to this technology can serve as a conductive and oxide prevention film and can be used to shield electromagnetic waves generated in high-density and high-power machines such as TVs, radios, computers, or video game consoles.

Moreover, the conductive paste composition is composed of environment-friendly components and can give electric features while suppressing formation of an oxide film when being used in a metal terminal or a gold terminal of high-end electronic appliances or electric appliances such as DVDs, TVs, and home theater systems, thereby maintaining and reproducing the original states of used products.

4. Applicable market and use of the technology

This technology relates to a conductive paste in which the ‘paste’ is a compound(dispersion) of an organic vehicle and powder(metal, glass, ceramic) applied to implement electric features required for electronic parts and devices.  The conductive paste does not has strong adhesive property because of being printed in a circuit board or a membrane sheet.

Presently, a circuit pattern in an electronic part such as a cellular phone is generally plated, resulting in the waste liquor problem.  As a result, a conductive paste is suggested as a substitute.  With the recent development of a nano paste made of nano particles of silver or copper, expectations of the conductive paste increase more and more.

Metal powder becomes more important as it is widely used to manufacture electric and magnetic materials, conductive pastes, batteries, high-temperature metal and ceramic complex materials, medical materials, and defense industry products.  Recently, super-powder synthesized by super-powdering technologies has superior functionality such as high rigidity by improving the density of a powder metallurgy part, thus attracting more and more attention.  In particular, due to features such as high heat resistance, super ferromagnetism, and multivalence, higher value-added metal powder can be realized by super-powering of cobalt powder applied in various industrial fields.