APPARATUS FOR MEASURING PEEL STRENGTH OF FABRIC

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 63 | 10-476077 | 2002-35857 | Korea Institute of Industrial Technology | G01N 3/00 |
| Registration 63 | 2005.03.02 | 2002.06.26 | Korea Institute of Industrial Technology | G01N 3/00 |
| Representative Fig. |

2. Summary of the technology

This technology relates to a device for measuring exfoliation strength necessary to exfoliate an arbitrary first fabric layer from a fabric specimen formed of two or more layers of fabrics bonded to each other.

In conventional devices for measuring exfoliation strength, only maximum tensile load can be measured, but the variation of the tensile load caused according to the time applied to the fabric specimen cannot be measured.  Further, in case where each part of the fabric specimen has different states or in case where the bonding states of the parts of the fabric specimen are different, the variations of the tensile load caused according to the partial difference cannot be measured.  In addition thereto, the conventional device for measuring exfoliation strength has a relatively large volume to cause the installation area to be much restricted, and the device is very expensive, thereby making it hard to easily use.

According to this technology, thus, the device for measuring exfoliation strength can measure and display the load applied to the fabric specimen in real time by the electronic control of the operations of the whole parts thereof, thereby overcoming the defects the conventional one-shaft tension measuring device like Instron has had.

According to this technology, there is disclosed a device for measuring exfoliation strength necessary to exfoliate an arbitrary first fabric layer from a fabric specimen formed of two or more layers of fabric bonded to each other, the device comprising: a specimen mounting part having a moving gripper adapted to firmly hold one end of the first fabric layer at one end of the fabric specimen and a fixed gripper adapted to firmly hold one end of the other fabric layer of the first fabric layer; a load applying part adapted to apply tensile load to the moving gripper in parallel relation with the fabric specimen so as to allow the moving gripper to be distant from the fixed gripper; a load measuring part adapted to measure the tensile load applied between the first fabric layer and the other fabric layer in real time; and a control part adapted to control the whole operations and to receive the measured value from the load measuring part, wherein the load applying part comprises a motor, a belt for converting the rotary force of the motor into the tensile load, and a roller formed between the motor and the belt so as to transmit the rotary force of the motor to the belt, each of the moving gripper and the fixed gripper having upper and lower members pivoted to each other, at least one of the lower surface of the upper member and the upper surface of the lower member being knurled.

3. Characteristics and/or advantages of the technology

In the conventional devices for measuring exfoliation strength, only maximum tensile load can be measured, but in the device for measuring exfoliation strength according to this technology, a digital gauge is attached to measure the variation of the tensile load caused according to the time applied to the fabric specimen.

Also, the device according to this technology has an advantage in that more accurate measuring values can be obtained when compared with the conventional analog measurers.

Further, even in case where each part of the fabric specimen has different states or even in case where the bonding states of the parts of the fabric specimen are different, the variations of the tensile load caused according to the partial difference can be measured.

Moreover, the device according to this technology has a relatively small volume to cause the installation area to be less restricted, and the device has very low prices to allow the measuring to be carried out at any working sites.

Also, the fabric specimen can be easily mounted, thereby permitting the working convenience to be increased.

Furthermore, as the device according to this technology is connected to a computer, the data input, the measuring and the output of the measuring value are controlled remotely.

4. Applicable market and use of the technology

This technology relates to the device for measuring the bonding strength of two or more layers of fabrics bonded to each other in accurate and easy manners in a field of manufacturing outdoor wear fabrics, and especially, this technology is necessarily applied to the fields where the bonding strength of high performance of permeability, wind-proof, water-proof fabrics should be measured.