NITRIDING METHOD AND APPARATUS USING POST-PLASMA

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 43 | 10-610645 | 2004-111185 | Korea Institute of Industrial Technology | C23C 8/24 C23C16/50 |
| Registration 43 | 2006.08.02 | 2004.12.23 | Korea Institute of Industrial Technology | C23C 8/24 C23C16/50 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a method and apparatus for nitrification using post plasma in order to improve the nitrification performance of a specimen by means of pre-processing and by performing nitrification fast by using a nitrification accelerator and generating plasma in a screen net.

ㅇ	Conventional nitrification methods used as hardening technologies for beautiful looking of metal surface or for improvement of abrasion resistance, fatigue resistance, or corrosion resistance are gas nitrification, salt bath nitrification, ion nitrification, and post plasma nitrification.  However, these methods have some problems.

To solve the problems, this technology is an improved technology which provides a method and apparatus for nitrification using post plasma in order to improve nitrification performance by performing pre-processing for activating specimen surface before performing nitrification on the specimen.

ㅇ	The method according to this technology includes a surface activation process of when nitrating a specimen by charging the specimen into a furnace, heating the specimen, and causing gas to pass through the plasma generated outside the specimen, generating plasma in a screen net installed outside the specimen and removing gas and impurities remaining on the specimen surface by using oxidation and reduction gas, a nitrification layer forming process of injecting a nitrification agent having nitrogen, hydrogen, and a nitrification accelerator added thereto into the specimen passing through the surface activation process in order to nitrate the specimen, and a cooling process of cooling the specimen passing through the nitrification layer forming process by lowering the temperature of the furnace.

3. Characteristics and/or advantages of the technology

This technology relates to a nitrification method using nitrogen ionized in an atomic state, i.e., ATONA(Atomic Nitriding).  While a conventional plasma nitrification method results in a crystal grain of 1~2 ㎛ after processing, this technology results in a fine texture having a crystal grain size of 10~50 ㎛ after ATONA processing.  This result means that nano-size nitrification can be performed and thus nitrogen can be absorbed quickly and deeply over a large surface area.  Thus, according to this technology, high-quality thermal processing can be performed while reducing nitrification time without rigidity degradation within steel.

Moreover, post-processing such as coating can be performed without changes in color and processing surface after ATONA processing.  This technology can improve nitrification performance of specimen by optimal carbon-containing nitrification processing, improve nitrification properties of mold steel that is difficult to nitrate, and obtain superior illuminance.

Moreover, this technology increases energy density and temperature uniformity and improves the efficiency of nitrification by directly using active radicals passing through plasma.  Furthermore, since this technology does not directly apply glow to a target specimen, the surface of the specimen is not damaged and the shape of the specimen is not limited to particular shapes, thereby allowing simultaneous processing of various shapes of specimens and applying nitrification into narrow holes.

4. Applicable market and use of the technology

This technology is meaningful in that a thermal processing basic technology is innovated by solving conventional problems.  This technology can be applied to fast and precise processing of mold tools or low-temperature processing of vehicle parts, thereby significantly improving international competitiveness of corresponding parts.  In particular, along with quality improvement, the manufacturing costs of vehicle parts and precision mechanical parts can be reduced by a large amount, thereby attracting much attention from related businesses.

By applying this technology, lubrication coating called DLC(Diamond Like Carbon) having high adhesion and low friction coefficient with respect to vehicle piston rings, wet-operating parts, and air conditioner veins can be processed simply.

Since thermal processing is a core manufacturing process of mechanical parts, our rivals Japan and China can be easily driven away by this technology.  This is true because thermal processing is given a great deal of weight, e.g., 37 % of the entire processing in vehicle parts.

Moreover, mass production of carbon nano tube called 'dream new material' can be hastened by utilizing this technology.  This is because carbon nano tube using pure iron remaining on the steel surface as a catalyst can be obtained by reducing nitrogen and immediately injecting gas containing carbon such as ammonia gas after ATONA processing.