NANO INK JET PRINTER HEAD AND A MANUFACTURING METHOD THEREOF

1. Information of the paten

| Dowon International Administration Nos. | Registration Nos. | Application Nos. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration Nos. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 1 | 10-510777 | 2003- 70187 | Korea Institute of Industrial Technology | B41J 2/045 |
| Registration 1 | 2005.08.19 | 2003.10.09 | Korea Institute of Industrial Technology | B41J 2/045 |
| Registration 6 | 10-665928 | 2005-131981 | Korea Institute of Industrial Technology | B41J 2/ 01 |
| Registration 6 | 2007.01.02 | 2005.12.28 | Korea Institute of Industrial Technology | B41J 2/ 01 |
| Representative Figs. |

2. Summary of the technology

This technology relates to a nano ink jet printer head and a manufacturing method thereof, which is provided to easily process a hole having a diameter 10 nm or lower by utilizing a hydrodynamic focusing effect.

It has been a problem that the conventional nano ink jet printer head's hole is being blocked up while its standby status after spraying. Therefore, this technology is an improved one constructed such that ink is circulated continuously so as to preclude the ink from being hardened at the narrow nozzle and particulate through the re-circulation method of the ink when the printer head is not used and thus, is standby status.

A nano ink jet printer head according to the present technology is comprised of ink supply parts supplying the ink; air supply parts installed to supply air; ink re-circulation discharge parts connected to an ink storage; pressure chambers discharging the ink when pressed; an ink channel discharging the ink supplied from the ink supply part; air channels discharging the air supplied from the air supply part; a focusing part generating the ink-air flow; an ink discharge channel guiding the ink-air flow to the outside; and an ink re-circulation channel guiding the ink-air flow to the ink re-circulation discharge part.

3. Characteristics and/or advantages of the technology

According to this technology, it is features that nano ink jet printer head and method for manufacturing the same are provided without the processing a hole having a diameter 10 mn or lower by utilizing a hydrodynamic focusing effect to the nano ink jet technology used in the biotechnology field.

This technology also has an advantage in that it can be manufactured easily by simplifying the structures of the two upper and lower plates of a printer head being connected together and it can be manufactured small-sized product.

4. Applicable market and use of the technology

This technology relates to an ink jet printer head, and it can be applicable to companies that deal with the products of printer and are developing the related services in the market of this field.

This technology also relates to MEMS(Micro Electro Mechanical Systems), which is manufacturing method of ultra fined mechanical structure, for example, VLSI(Very Large Scale Integrated Circuit) made by processing of silicon, crystal, glass, etc, micro-mini gear that is half thickness of a hair, and nail-sized hard disc, etc. The micro-mini mechanical product made by the MEMS technology has an accuracy of less than a micrometer(10-6m). And, it makes possible to mass production of micro-mini product with lower cost by applying fine processing technology of semiconductor that repeats evaporation and etching process in the structural aspect and also makes possible to reduce power consumption amount by applying the principle of generating electric current, for example, static electricity that pulls between electric charges and surface tension in a driving power aspect. There are now growing attention and importance about afore said technologies with the introduction of nano and SoC(System on Chip) technologies. MEMS is the best promising technology in the 21st century, and is as prospective as semiconductor, which is the 20th century's representative technology. Currently, technological coverage of MEMS can be extended not only to acceleration sensor for a car air bag and ink jet printer head, but also dramatically to the minute mechanical product, for example, bio-medical science, especially biochip for decoding genetic information, wireless component, optical parts, and so on.