TIRE CODE ADHESIVE COMPOSITION INCLUDING BLOCKED ISOCYANATE COMPOUND

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 36 | - | 2007-64857 | Korea Institute of Industrial Technology | C08K 5/3415 |
| Application 36 | - | 2007.06.29 | Korea Institute of Industrial Technology | C08K 5/3415 |
| Representative Fig. |

2. Summary of the technology

ㅇ	This technology relates to a tire code adhesive composition including a blocked isocyanate compound.

ㅇ	A tire code adhesive necessarily uses a crosslink agent for maintaining a strong and stable(high-temperature resistance and fatigue resistance) adhesive force in a harsh environment(typically at 300 ℃ or higher and during long-time fast driving).  Thus, there has been steady demand for a blocked isocyanate compound generally used as a crosslink agent.  A blocking agent for manufacturing the crosslink agent inevitably is deposited and remains in a tire code after cross-linking in the form of impurities.

Moreover, there have been demands for blocked isocyanate having a new function and a complex function without degradation in physical properties of a substrate.

This technology is an improved technology for reducing hardening time without using a separate vulcanization accelerator by using a new blocking agent and improving physical properties of a tire code while the dissociated blocking agent after used remaining within a tire code.

ㅇ	This technology is composed of a tire code adhesive composition including a blocked isocyanate compound expressed by chemical formula 1(refer to the above representative figure).

3. Characteristics and/or advantages of the technology

This technology is characterized in that a dissociated blocking agent after used remains within a tire code and rather improves physical properties of the tire code than serves as impurities.

In addition, this technology has a feature that blocked isocyanate used as a crosslink agent for manufacturing a tire code adhesive has a vulcanization acceleration effect, removing a need for a separate vulcanization accelerator.

Therefore, this technology is economical in terms of reductions in raw material cost, manufacturing cost, and processing steps owing to the non-use of a separate vulcanization accelerator.

Moreover, blocked isocyanate according to this technology enhances mechanical properties(high rigidity, high elasticity, low contractibility) of a tire code and heat resistance.

4. Applicable market and use of the technology

This technology is useful in various home and industrial fields where blocked isocyanate is used as a water repellent agent and a coupling agent as well as a tire code crosslink agent and in industrial fields requiring improvement of physical properties of a tire code.