34. Food packing film having antioxidizing and antibacterial characteristics and method of manufacturing the same

| Ⅰ |  | Analysis of Technical Trend |
| --- | --- | --- |

1. Summary of Technology

| Definition |  | The present invention relates to a functional polyethylene film for food packing material and a method of manufacturing the same, and more particularly, to a functional polyethylene film for food packing material, which has both antioxidizing and antibacterial properties by properly using an antioxidant and antibiotics which can be safety used as the constituent raw material of food packing material, and a method of manufacturing the same. |
| --- | --- | --- |
|  |  | The present invention relates to a functional polyethylene film for food packing material and a method of manufacturing the same, and more particularly, to a functional polyethylene film for food packing material, which has both antioxidizing and antibacterial properties by properly using an antioxidant and antibiotics which can be safety used as the constituent raw material of food packing material, and a method of manufacturing the same. |
| Keyword |  | antibacterial, antioxidizing, polyethylene, packing |
|  |  | antibacterial, antioxidizing, polyethylene, packing |
| Related Figure |  | 항산화성분: Antioxidizing components (tocopherol, TBHO, etc.) PE 혼합: Mix PE 압출: Extraction 냉각: Cool 절단: Cut 항산화용 PE 마스터 배치: Place PE master for antioxidization 항균성분: Antibiotic material (chitosan) 전처리가공: Pre-processing PE 혼합: Mix PE 압출: Extraction 냉각,절단: Cool and cut 항산화용 PE 마스터 배치: Place PE master for antioxidization PE 혼합: Mix PE 압출가공: Extraction process 나일론 접착: Adhere nylon 포장용 필름: Packing film | Diagram showing a process of manufacturing a polyethylene film having antioxidizing and antibacterial characteristics according to the present invention |
|  |  | 항산화성분: Antioxidizing components (tocopherol, TBHO, etc.) PE 혼합: Mix PE 압출: Extraction 냉각: Cool 절단: Cut 항산화용 PE 마스터 배치: Place PE master for antioxidization 항균성분: Antibiotic material (chitosan) 전처리가공: Pre-processing PE 혼합: Mix PE 압출: Extraction 냉각,절단: Cool and cut 항산화용 PE 마스터 배치: Place PE master for antioxidization PE 혼합: Mix PE 압출가공: Extraction process 나일론 접착: Adhere nylon 포장용 필름: Packing film | Diagram showing a process of manufacturing a polyethylene film having antioxidizing and antibacterial characteristics according to the present invention |
| Technical Characteristics & Merit |  | An antioxidizing and antibacterial functional film for food packing according to the present invention is used as sanitary packing materials for various food, which are easily exposed to oxidization and bacterial corruption, thereby significantly improving acidification deterioration and browning of food, and a reduction in freshness and a corruption phenomenon caused by increased bacteria. It was found that a sample packed using the film for packing according to the present invention had the number of microogranisms after a lapse of 15 days reached 3.3 x 105/g, so it was recognized that there is an effect of prohibiting an increase of microogranisms by 300 % or more when compared with general PE films. |
|  |  | An antioxidizing and antibacterial functional film for food packing according to the present invention is used as sanitary packing materials for various food, which are easily exposed to oxidization and bacterial corruption, thereby significantly improving acidification deterioration and browning of food, and a reduction in freshness and a corruption phenomenon caused by increased bacteria. It was found that a sample packed using the film for packing according to the present invention had the number of microogranisms after a lapse of 15 days reached 3.3 x 105/g, so it was recognized that there is an effect of prohibiting an increase of microogranisms by 300 % or more when compared with general PE films. |

2. Present Status of Intellectual Property

| Country | Right | Status | Application No. (Filing Date) | Registration No. (Registration Date) |
| --- | --- | --- | --- | --- |
| Korea | Patent | Registered | 10-2004-0076660 (2004.09.23) | 10-0656984-0000 (2006.12.06) |
| Title of Invention | Food packing film having antioxidizing and antibacterial characteristics and method of manufacturing the same |

| Ⅱ |  | Analysis of Market Trend |
| --- | --- | --- |

1. Summary of Applicable Market

| Summary of Industry |  | The packing industry has high dependency on the manufacturing industry and has a great influence by a change in the manufacturing industry because it has an intermediate product industry characteristic like general components or the material industry input to the final goods production. In most countries including advanced countries, a slight difference exists depending on the volume or percentage of the manufacturing industry, but the fact that the packing industry occupies a constant percentage (about 1 % of the GDP)in the entire country shows that the packing industry has a high dependency on the internal industry. An industry structure based on small and medium enterprises reveals that internal resources or ability, in particular, technical development resources or ability are weak. In the packing industry of advanced countries, there is a tendency that technical competitiveness becomes enhanced because a price competition with developing countries based on a low wage is no longer possible. The supply chain of the packing industry includes packing material manufacturing companies, packing goods production and processing companies, packing machine companies, packing related service companies, distribution companies (wholesale and retail sale companies), and manufacturing companies. A technical reform in a functional film has satisfied needs in terms of the need, and the production line of the film industry has been expanded, thereby making smooth the supply. |
| --- | --- | --- |
|  |  | The packing industry has high dependency on the manufacturing industry and has a great influence by a change in the manufacturing industry because it has an intermediate product industry characteristic like general components or the material industry input to the final goods production. In most countries including advanced countries, a slight difference exists depending on the volume or percentage of the manufacturing industry, but the fact that the packing industry occupies a constant percentage (about 1 % of the GDP)in the entire country shows that the packing industry has a high dependency on the internal industry. An industry structure based on small and medium enterprises reveals that internal resources or ability, in particular, technical development resources or ability are weak. In the packing industry of advanced countries, there is a tendency that technical competitiveness becomes enhanced because a price competition with developing countries based on a low wage is no longer possible. The supply chain of the packing industry includes packing material manufacturing companies, packing goods production and processing companies, packing machine companies, packing related service companies, distribution companies (wholesale and retail sale companies), and manufacturing companies. A technical reform in a functional film has satisfied needs in terms of the need, and the production line of the film industry has been expanded, thereby making smooth the supply. |
| Definition and Scope of Market |  | This technology can be applied to a variety of food, meat and fishes, and packing manufacturing companies such as food packing materials, detergent types, fiber tanning products, shampoo liquid phase, and so on. |
|  |  | This technology can be applied to a variety of food, meat and fishes, and packing manufacturing companies such as food packing materials, detergent types, fiber tanning products, shampoo liquid phase, and so on. |

2. Characteristics of Market

| Market Scale |  | The total production and the total value-added price of the local packing industry in 2005 were about 15 trillion won and about 6.1 trillion won. In the ratios occupied by the respective materials in the packing industry field, paper/board was 40~42 %, plastic container films were 35~38 %, metal was 10~12 %, glass was 5~8 %, and others including woods was 7~8 %. The sale of packing materials in 2005 was estimated to be about 5 trillion won, which was about 1/3 of the total volume of the packing industry, and the sales amount of the packing container industry was estimated to be about 10 trillion won. In the average growth rate of the local packing industry during the years 1999～2004, the production was about 9 % and a value-added amount was 7.2 %. It is expected that the global packing market volume will increase by 3.5 % annually, reaching 424 billion dollars in 2004 and 597 billion dollars in 2014. It is expected that the global packing market will see a growth rate of 3∼5 % during the next 5 years, and the functional film market will lead the market. |
| --- | --- | --- |
|  |  | The total production and the total value-added price of the local packing industry in 2005 were about 15 trillion won and about 6.1 trillion won. In the ratios occupied by the respective materials in the packing industry field, paper/board was 40~42 %, plastic container films were 35~38 %, metal was 10~12 %, glass was 5~8 %, and others including woods was 7~8 %. The sale of packing materials in 2005 was estimated to be about 5 trillion won, which was about 1/3 of the total volume of the packing industry, and the sales amount of the packing container industry was estimated to be about 10 trillion won. In the average growth rate of the local packing industry during the years 1999～2004, the production was about 9 % and a value-added amount was 7.2 %. It is expected that the global packing market volume will increase by 3.5 % annually, reaching 424 billion dollars in 2004 and 597 billion dollars in 2014. It is expected that the global packing market will see a growth rate of 3∼5 % during the next 5 years, and the functional film market will lead the market. |
| Market Trend |  | It is expected that the global high value-added industries, such as pharmacy industry, cosmetics industry, and electronic/electrical industry will continue to develop, and the packing market requiring these industries will continue to expand and develop. |
|  |  | It is expected that the global high value-added industries, such as pharmacy industry, cosmetics industry, and electronic/electrical industry will continue to develop, and the packing market requiring these industries will continue to expand and develop. |