WHITE ORGANIC LUMINESCENT DEVICE

1. Information of the patent

| Dowon International Administration No. | Registration No. | Application No. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration No. | Date of registration | Date of filing | Rightful institution | Remarks |
| Application 68 | - | 2007-72321 | Korea Institute of Industrial Technology | H05B 33/10 |
| Application 68 | - | 2007.07.19 | Korea Institute of Industrial Technology | H05B 33/10 |
| Representative Fig . |

2. Summary of the technology

ㅇ	This technology relates to a high luminance and high efficiency white organic luminescent device in which a guest dopant is partially doped into two different host materials on the basis of a dual part dye doping according to the International Commission on Illumination(CIE) coordinate(0.33, 0.33).

ㅇ	A conventional white organic luminescent device was problematic in that it had a limited performance according to characteristics of a  luminescent material and a severe change in luminescent color coordinates according to the intensity of an electric field. Thus, this technology is an improved technology, which can improve color coordinate movement according to a driving voltage and acquire a white organic luminescent device with improved luminance and efficiency, by solving the above disadvantages and problems of the conventional technology.

ㅇ	A white organic luminescent device of this technology is a technology, including a substrate a first electrode provided on the substrate; a charge injection layer provided on the first electrode a charge transport layer provided on the charge injection layer a luminescent layer provided on the charge transport layer and having a guest dopant doped therein to a specific thickness from a top surface; a charge transport layer provided on the luminescent layer and having the same guest dopant as the guest dopant doped into the luminescent layer to a specific thickness from an interface with the luminescent layer; and a second electrode provided on the charge transport layer.

3. Characteristics and/or advantages of the technology

This technology is characterized in that it can satisfy the safety of color with respect to high luminance, efficiency and a driving voltage and an equivalent energy, which complies with an approximate white point(x=0.33, y=0.33) on the standard chromaticity coordinate of the CIE.

This technology is advantageous in that it can control the CIE coordinate using an equivalent energy white point by doping one guest into two different hosts and can improve efficiency.

4. Applicable market and use of the technology

This technology is a technology regarding an organic luminescent device.  Technologies for implementing blue, red and green displays have generally been developed.  In recent years, continuous research has been done to white organic luminescent devices because of various possibilities of the white organic luminescent devices.  White organic luminescent devices of 20 to 30 lm/W have recently been issued, and a possibility that the white organic luminescent devices can be used as lightings along with luminescent diodes has emerged.

The organic luminescent device of this technology is a device that will be widely used for backlight of the next-generation displays and LCDs and lightings.  Active research has been done to the organic luminescent device.  The organic luminescent device can be applicable to full-color displays and lighting industry through a combination of a LCD color filter.