WIDE WIDTH COMPLEX COATING APPARATUS AND PROCESS EMPLOYING ELECTROMAGNETIC AND ULTRASONIC WAVE; and COMPOSITE COATING APPARATUS FOR WIDE AREA ULTRASONIC COATING AND SPIN COATING AND COATING METHOD THEREOF CAPABLE OF PREVENTING AIR TRAPPING IN FINE PATTERN AND REDUCING DEFECTIVE PROPORTION

1. Information of the patent

| Dowon International Administration Nos. | Registration Nos. | Application Nos. | Rightful institution | Remarks |
| --- | --- | --- | --- | --- |
| Dowon International Administration Nos. | Date of registration | Date of filing | Rightful institution | Remarks |
| Registration 67 | 10-749068 | 2005-131993 | Korea Institute of Industrial Technology | H01L 21/20 |
| Registration 67 | 2007.08.07 | 2005.12.28 | Korea Institute of Industrial Technology | H01L 21/20 |
| Registration 68 | 10-749037 | 2005-132384 | Korea Institute of Industrial Technology | H01L 21/02 |
| Registration 68 | 2007.08.07 | 2005.12.28 | Korea Institute of Industrial Technology | H01L 21/02 |
| Representative Figs. |

2. Summary of the technology

ㅇ	This technology relates to a wide width ultrasonic spray coating process, which can replace a spin-coating process used to coat a sensitizing solution, an etchant, an ITO coating agent, etc. on a semiconductor wafer or a display substrate, and a wide width ultrasonic wave and electromagnetic complex process and a fabrication apparatus thereof, in which sprayed particles are electrified and spray particles electrified by an adequate electromagnetic field is coated on a to-be-coated material to a more uniform thickness in order to effectively improve the efficiency of the process.

ㅇ	This technology is an improved technology that has improved a problem in which, in a process of coating a coating solution, which must be coated on a surface of a substrate, a wafer or a similar to-be-coated material through high-speed spin rotation in an existing spin process method, the coating solution is scattered and an unnecessary amount of the coating solution is consumed, causing environmental problems and loss of the material, disadvantages in which air is not discharged from patterns or rugged portions on a wafer in a spin method and a coating solution or an etchant is coated thereon, so defects are likely to occur in products in a subsequent multi-step process, and expenses for an apparatus necessary for high-speed rotation when coating a desired coating solution on a large-sized substrate are increased, and a problem in which it is difficult to uniformly control a coating thickness on a large-sized substrate.

ㅇ	The wide width complex coating apparatus and process employing electromagnetic field and ultrasonic waves of this technology are technologies regarding a coating apparatus for coating a sensitizing solution, an etchant, an ITO coating agent or the like on a semiconductor wafer,  a display substrate, etc., including a liquid supply device for supplying a coating agent; an ultrasonic wave nozzle for spraying samples by atomizing the coating agent supplied from the liquid supply apparatus; a discharge device for electrifying the atomized particle sprayed from the ultrasonic wave nozzle and an electromagnetic excitation device for exciting the atomized particle coated on the sample electromagnetically.

3. Characteristics and/or advantages of the technology

This technology is characterized in that it can save apparatus expenses and environment cost by mixing an electromagnetic electrifying method while employing an ultrasonic wave coating method with less installation and maintenance cost, does not have defects such as air bubbles, and can obtain a uniform coating result.

This technology is advantageous in that it can reduce the scattering of a coating solution and minimize environmental problems and loss of the material in the process of coating the coating solution, which must be coated on a surface of a substrate, a wafer or a similar to-be-coated material.

This technology is characterized in that it can obtain a more uniform thickness of a coating material by integrating a wide width ultrasonic spray coating process, which can replace a spin-coating process used to coat a sensitizing solution, an etchant, an ITO coating agent, etc. on a semiconductor wafer or a display substrate, and an electromagnetic excitation apparatus for improving the efficiency of the process more effectively, and is advantageous in that it provides a cheap high efficiency and environment-friendly coating process and a fabrication apparatus thereof, which can increase the coating speed and reduce the size of a fabrication line.

4. Applicable market and use of the technology

This technology is a technology used to coat a sensitizing solution, an etchant, an ITO coating agent, and so on a semiconductor wafer, a display substrate, etc. and can be widely used for companies such as semiconductor wafer production companies, display substrate production companies, and so on.